NATIONAL OCCUPATIONAL STANDARD

Marble Natural Stone Surface Treatment Worker

LEVEL 3

REFERENCE CODE / …

OFFICIAL JOURNAL DATE-ISSUE/ …

| Occupation: | Marble Natural Stone Quarry Worker |
| --- | --- |
| Level: | 3 Qualification level of the occupation has been determined as level (..) in octal (8) level matrix. |
| Reference Code: | ……………………………………. |
| Prepared by: | ………………………………………… |
| Verified by: | VQA ………. Sector Committee |
| VQA Board of Directors Approval Date/Issue: | ………… Date and Decision No.………. |
| Official Gazette Date / Issue: | … |
| Revision No: | 00 |

TERMS, SYMBOLS AND ABBREVIATIONS

BLOCK: Properly shaped mass which has economic value and obtained from marble blocks

NATURAL STONE: It is the name given to rocks formed naturally in nature which can take any shape using specific hand tools in the decorative way, on which all kinds of surface treatment can be performed, which can be polished and cut, and given corner and edge when cut, and which permit taking blocks whatever their style of formation.

OHS: Occupational Health and Safety

PERSONAL PROTECTIVE EQUIPMENT (PPE): All kinds of tools, instruments, appliances and devices which are worn, put on or hold by the worker and which protect the worker from one or more hazards arise from the work and effect the health and safety of the worker, and which were designed to suit such purpose,

MARBLE: Marble is the rock formed as a result of the re-crystallisation of lime stones combined with Calcium Carbonate or Magnesium Calcium by metamorphosing under the effect of pressure and temperature.

WASTE: Pieces of marble or natural stone which cannot be utilized as block and rubble at the quarry

WASTE DISPOSAL AREA: Specific are for disposal of waste

RISK: The composition of the possibility of any dangerous situation and the results of the same,

DANGER: Potential of damage or injury likely to affect the worker or work place and likely to exist in the workplace or to be caused externally,

SAW: Stone cutting disc with a steel body in different sizes and thicknesses, which is surrounded by stone cutting apparatus called sockets that are attached to the body of the saw by welding,

TILE: Material in different sizes, which is produced from all kinds of natural stones, has the thickness of 1-1.2-1.5 cm, under which joint gap is opened, and four sides of which is chamfered, and which is pasted while performing wall covering work,

PALLET: Wooden material, on which substances are collected and which is produced in a way that ensures to be carried easily by forklift

CONVEYOR: The band which has a definite size, is made of rubber-plastics mixture material, and which automatically carries the marble tablets placed on it

STRIP: Marble and natural stone tablets which are cut in definite length and thickness

PLATE: Block shaped marble or natural stone tablets, which have geometric shapes and different sizes, and which are cut in different thicknesses

TABLET: Marbles or natural stones with definite thicknesses, sizes and geometric shapes,

GRAPPLING TOOL: A steel tool used to grapple, lift and move the big marble plates, which compresses more by moving in the opposite sides due to the plate weight, and inner parts of which are covered with rubber,

CONTROL PANEL: Electronic panel, which is furnished with several buttons, and which is used to digitally record the values to be given according to the production details of the machines, and to perform the process in accordance with the records

JOINT GAP: Approximately 1 mm or deeper gap, which is grooved in the bottom surface of the tile in order to paste it

CHAMFER: The procedure of removing the sharp-pointedness of the edges of marble and natural stone tablets

TABLE OF CONTENTS

1.	INTRODUCTION	6

2.	INTRODUCTION OF THE OCCUPATION	7

2.1.	Definition of the Occupation	7

2.2.	Place of the Occupation in International Classification System	7

2.3.	Regulations on Health, Safety and Environment	7

2.4.	Other Legislation regarding the Occupation	7

2.5.	Working Environment and Conditions	8

2.6.	Other Requirements regarding the Occupation	8

3.	OCCUPATIONAL PROFILE	9

3.1.	Duties, Tasks and Performance Criteria	9

3.2.	Tools, Appliances and Equipment Used	23

3.3.	Knowledge & Skills	23

3.4.	Attitudes and Behaviors	24

4.TESTING, ASSESSMENT AND CERTIFICATION	26

1.	INTRODUCTION

National occupational standard titled Marble Natural Stone Surface Treatment Worker (Level 3) was issued by Turkish Association of Marble, Natural Stone and Machine Producers (TÜMMER) assigned as per the provisions of Vocational Qualifications Authority (VQA) Law No.5544 and “Bylaw on Drawing up National Occupational Standards” and “Regulation on the Establishment, Duties and Operation Procedures and Principles of the Sector Committees of Vocational Qualification Authority” introduced pursuant to the aforementioned Law.

National occupational standard titled Marble Natural Stone Surface Treatment Worker (Level 3) was assessed upon receiving the opinions of the related institutions and organizations in the sector, and approved by VQA Board of Directors upon examination of VQA Mining Sector Committee.

2.	INTRODUCTION OF THE OCCUPATION

2.1.	Definition of the Occupation

Marble Natural Stone Surface Treatment Worker (level 3); is a qualified person who organizes the work, polishes the surfaces of marble natural stone, applies marble natural stone surface treatment procedures such as honing, sanding, brushing, hammering, indentation, filling, surface polishing, burning, acid treatment, and ageing, and who attends vocational development activities.

2.2.	Place of the Occupation in International Classification System

ISCO 08 : 7113 Stonemasons, stone cutters and carvers

2.3.	Regulations on Health, Safety and Environment

Social Security and General Health Insurance Law No.5510

Regulation on Heavy and Dangerous Work, By-Law on Occupational Health and Safety, Regulation on Conditions of Health and Safety in Using Work Equipment, Regulation on Use of Personal Protective Equipments in the Workplace, Regulation on Safety and Health Signs

Regulation on Heavy and Dangerous Work, Communication on Vocational Training of Workers in Heavy and Dangerous Work

Regulation on the general Principles of Waste Management

Regulation on Procedures and Principles of Occupational Health and Safety Trainings of the Employees

Regulation on Health and Security Measures for Working with Devices with Screens

Regulation on Manual Handling Works

Regulation on Noise

Regulation on Preparation, Completing and Cleaning Works

Occupational Safety and Health Regulation

Regulation on Health and Safety Measures to be taken in the Workplace Buildings and Additional Buildings

Regulation on Control of the Solid Wastes

Regulation on Preventing the Personnel from the Hazards of the Explosive Environments

Regulation on Fire

And, it is essential to obey laws, rules and regulations on occupational health and safety and environment; and to perform risk analysis regarding this issue.

2.4.	Other Legislation regarding the Occupation

Labor Act No.4857

Social Security and General Health Insurance Law No.5510

Law on Quarry No.3217

Environmental Law No.2872

Furthermore, it is essential to obey other current legislations, laws, statutory rules and by-laws concerning the occupation.

2.5.	Working Environment and Conditions

Marble Natural Stone Surface Treatment Worker (level 3) works at appropriate temperature in open or closed factory environment that includes machines working with a large quantity of water, which is adequately lighted, humid, dusty, and noisy; and where occupational health and safety measures are required to be taken. S/he works in communication with his/her co-workers and relevant authorities, depending on the requirements of work; works almost any time of the year as long as atmospheric conditions are convenient; mostly is on the move in the process of work and sometimes must stand on feet for a long time and carry heavy materials; may face occupational diseases like backache, knee pain, rheumatism diseases etc. due to the environmental conditions, and uses appropriate personal protective equipment during the procedures. There are also damage and injury risks which require taking occupational health and safety measures while practicing the work.

2.6.	Other Requirements regarding the Occupation

Marble Natural Stone Surface Treatment Worker (level 3) must have the “Form of Initial Entrance and Periodical Medical Examination for Workers in Heavy and Dangerous Works”.

3.	OCCUPATIONAL PROFILE

3.1.	Duties, Tasks and Performance Criteria

| Duties | Tasks | Performance Criteria |
| --- | --- | --- |
| Code | Title | Code | Title | Code | Description |
| A | To take precautions related to quality, environmental safety and occupational health and safety | A.1 | To be informed of and to participate in trainings/ meetings of environment and OSH | A.1.1 | Participates in internal training activities to improve his/her knowledge on work experience and in external training activities if charged. |
|  |  |  |  | A.1.2 | Does what is required in accordance with the information s/he received and determined before, makes recommendations. |
|  |  |  |  | A.1.3 | Informs and demands his/her superiors on training subjects s/he identified related to work. |
|  |  |  |  | A.1.4 | Participates in trainings organized according to requirements. |
|  |  |  |  | A.1.5 | Tries to provide maximum benefits for his/her own personal development from trainings. |
|  |  |  |  | A.1.6 | Identifies acquisitions from trainings s/he participated, gives feedback. |
|  |  | A.2 | To take precautions against risks and hazards | A.2.1 | Learns and complies with the information s/he received related to risks and hazards to be raised in work environment. |
|  |  |  |  | A.2.2 | Attends to the studies conducted to evaluate the risk factors and obtains information and skills for reducing the same. |
|  |  |  |  | A.2.3 | Learns and complies with the important information s/he received for safety at work. |
|  |  |  |  | A.2.4 | Learns and complies with the information s/he received for situations requiring emergency action and having importance in the aspect of work safety, participates in practices. |
|  |  |  |  | A.2.5 | Learns the information related to personal protective equipment required for work and use of this equipment, and complies with this information. |
|  |  |  |  | A.2.6 | Learns, complies and applies information s/he received on safe use of machines and equipments required for work. |
|  |  |  |  | A.2.7 | Learns the meaning of table and signs which are required to be present at work environment and acts in compliance with such rules. |
|  |  |  |  | A.2.8 | Complies with the directives prepared on environment and work safety, acts in compliance with such rules. |
|  |  |  |  | A.2.9 | Obeys the directives on use of work area clearly, orderly and in conformity with hygienic rules, acts in compliance with these rules, and warns those who do not obey such rules. |
|  |  |  |  | A.2.10 | Makes appropriate controls in compliance with the instructions of technical supervisor and occupational health and safety specialist on equipments which are on his/her own disposal and responsibility at work area and on connection of this equipment to all system. |
|  |  | A.3 | To notify concerned people of deficiencies on environment and OHS | A.3.1 | Notifies deficiencies related to OHS and environment as insufficient lighting, warning sign and protective equipment which may imperil worker's safety at work, follows up until these deficiencies are resolved. |
|  |  |  |  | A.3.2 | Notifies concerned people in written of non resolved deficiencies. |
|  |  |  |  | A.3.3 | Identifies equipments and appliances which imperil his/her safety and which are in his/her personal use and demands improvement, change or renewal. |
|  |  |  |  | A.3.4 | Pays attention to equipment required for emergency case is ready and available. |

| Duties | Tasks | Performance Criteria |
| --- | --- | --- |
| Code | Title | Code | Title | Code | Description |
| B | To organize the work (To be continued) | B.1 | To take over shift | B.1.1 | Obtains information on instructions about works or problems which will affect them from former shift production staff. |
|  |  |  |  | B.1.2 | Applies operating procedures related to shift takeover. |
|  |  |  |  | B.1.3 | Takes order from his/her superiors related to works to be performed at the beginning of his/her shift. |
|  |  | B.2 | To record works performed | B.2.1 | Writes properly all operating procedures, information of team participated in work, material used, definition of work in related forms. |
|  |  |  |  | B.2.2 | Delivers this form and records to his/her superiors by signing. |
|  |  | B.3 | To plan works under his/her duty | B.3.1 | Plans his/her works according to their duration and content of application, by sequencing the works to be performed in his/her shift according to work orders given by his/her superiors. |
|  |  |  |  | B.3.2 | Confirms this planning within the frame of his/her works with his/her superiors. |
|  |  | B.4 | To provide appliances, material and equipment | B.4.1 | Determines appliances, consumable material and equipments suitable for his/her works to be performed according to their quantity and functionality. |
|  |  |  |  | B.4.2 | If appliances, material and equipment required for the work are found at the storage unit, s/he provides them from there. |
|  |  |  |  | B.4.3 | Resolves deficiencies by controlling cleaning and maintenance of the equipments. |
|  |  |  |  | B.4.4 | Keeps clean and tidy all storage units and lockers. |
|  |  |  |  | B.4.5 | Reports all equipment deficiencies and failures, condition of his/her material required for operation if they are decreased or not available to his/her superiors. |

| Duties | Tasks | Performance Criteria |
| --- | --- | --- |
| Code | Title | Code | Title | Code | Description |
| B | To organize the work | B.5 | To hand over shift | B.5.1 | Records the condition of systems at working area, the problems likely to affect the next shift, and the interventions done and likely to be done concerning these problems, on the shift log according to the operating procedures. |
|  |  |  |  | B.5.2 | Makes explanations in compliance with the instructions to next shift's production staff on issues recorded in shifts book. |

| C | To polish the surface of marble natural stone | C.1 | To furnish the surface of plate tablet | C.1.1 | Places the plate tablets, which were cut, on the plate polishing machine, using vacuum jib crane, leaves equal space at two sides. |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | C.1.2 | Checks the grinding stones of the thickness calibration heads of the polishing machine. |
|  |  |  |  | C.1.3 | Replaces the functionless ones. |
|  |  |  |  | C.1.4 | Checks the polishing stones of the polishing heads, and replaces the functionless ones. |
|  |  |  |  | C.1.5 | Turns on the fresh water valve, and sprays water on the polishing surface. |
|  |  |  |  | C.1.6 | Runs the machine, ensures that the heads turn in a constant speed. |
|  |  |  |  | C.1.7 | Directs the plate tablet under the heads. |
|  |  |  |  | C.1.8 | Adjusts the pressure to be applied on the surface of the stone by calibration and polishing heads to 200 bars, and ensures that they descend on the surface of the stone. |
|  |  |  |  | C.1.9 | Ensures the automatic conveyor band to run at an adequate polishing speed. |
|  |  |  |  | C.1.10 | Receives the stone, surface of which is polished, from the exit point and checks it. |
|  |  |  |  | C.1.11 | Directs the stone to the next point of procedure, if the polishing procedure is completed. |
|  |  |  |  | C.1.12 | Directs the stone to the polishing line again, provided that there are some deficiencies in polishing. |
|  |  | C.2 | To polish strip or sized tablets | C.2.1 | Removes the head covers of the polishing machine, and examines the heads one by one. |
|  |  |  |  | C.2.2 | Replaces the finished polishing stones. |
|  |  |  |  | C.2.3 | Enters the settings of the calibration and polishing heads to the machine, according to the thickness of the stone to be polished and part of the stone to be grinded. |
|  |  |  |  | C.2.4 | Adjusts the forward move speed of the strip. |
|  |  |  |  | C.2.5 | Adjusts the pressure to be applied on the surface of the stone by calibration and polishing heads to 200 bars, and ensures that they descend on the surface of the stone. |
|  |  |  |  | C.2.6 | Places the stones to be polished to the polishing opening. |
|  |  |  |  | C.2.7 | Turns on the fresh water spraying valve, on the band. |
|  |  |  |  | C.2.8 | Ensures the band to move, starts the polishing procedure. |
|  |  |  |  | C.2.9 | Observes the calibration and polishing heads through the open covers, throughout the polishing procedure, and checks how they work. |
|  |  |  |  | C.2.10 | Checks the polishing of the strips or sized tablets that came to the end of the band as the polishing procedure is over. |
|  |  |  |  | C.2.11 | Directs the stone to the next point of procedure, if the polishing procedure is completed. |
|  |  |  |  | C.2.12 | Directs the stone to the polishing line again, provided that there are some deficiencies in polishing. |

| D | To treat marble natural stone surfaces | D.1 | To hammer | D.1.1 | Contributes to bringing the plates, strips, and sized tablets, to be treated by hammering, to the feeding part of the hammering machine. |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | D.1.2 | Checks the hammer components of the machine. |
|  |  |  |  | D.1.3 | Replaces the hammers that are unable to perform treatment. |
|  |  |  |  | D.1.4 | Adjusts the impact intensity, which is to be applied by the hammers to the surface of the stone. |
|  |  |  |  | D.1.5 | Gives forward movement to the machine band. |
|  |  |  |  | D.1.6 | Turns on the fresh water spraying valve, on the stone. |
|  |  |  |  | D.1.7 | Runs the machine, and performs the hammering procedure. |
|  |  |  |  | D.1.8 | Receives the stones from the outlet point, and checks them. |
|  |  |  |  | D.1.9 | Places the stone on pallet, and directs them to the next procedure point. |
|  |  | D.2 | To perform chamfer procedure | D.2.1 | Contributes to bringing the strips or sized tablets, to the machine usage area. |
|  |  |  |  | D.2.2 | Installs the related apparatus to the machine, according to the chamfer type to be applied. |
|  |  |  |  | D.2.3 | Places the tablets on the band. |
|  |  |  |  | D.2.4 | Turns on the valve for spraying water, on the band. |
|  |  |  |  | D.2.5 | Starts the chamfer procedure, by moving the band forward. |
|  |  |  |  | D.2.6 | Checks the treated tablets, and places them on the pallet. |
|  |  | D.3 | To sand | D.3.1 | Contributes to bringing the plates, strips, and sized tablets, to be treated by sanding, to the feeding part of the sanding machine. |
|  |  |  |  | D.3.2 | Adjusts the air pressure of the sanding machine. |
|  |  |  |  | D.3.3 | Adjusts the size of the sand, and fills the sand tank. |
|  |  |  |  | D.3.4 | Sets the spraying time and range, as well as the speed of the band, according to the pattern to be applied on the surface. |
|  |  |  |  | D.3.5 | Places the material to be sanded on the band. |
|  |  |  |  | D.3.6 | Runs the machine, moves the band, and performs the sanding procedure. |
|  |  |  |  | D.3.7 | Receives the sanded material from the outlet of the machine. |
|  |  |  |  | D.3.8 | Turns the stone, and removes the sands and the particles on the surface sanded. |
|  |  |  |  | D.3.9 | Places the sanded stones on pallet, and directs them to the next procedure point. |

|  |  | D.4 | Honing | D.4.1 | Opens the head covers of the honing machine. |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | D.4.2 | Checks the status of calibration grinding head stones. |
|  |  |  |  | D.4.3 | Replaces the functionless ones. |
|  |  |  |  | D.4.4 | Checks the status of the honing heads. |
|  |  |  |  | D.4.5 | Replaces the honing stones that are unable to perform any treatment. |
|  |  |  |  | D.4.6 | Adjusts the pressure to be applied on the surface of the stone by the calibration and honing heads to 200 bars. |
|  |  |  |  | D.4.7 | Turns on the fresh water spraying valve, and sprays water to the surface. |
|  |  |  |  | D.4.8 | Runs the machine, and adjusts the spinning speed of the heads. |
|  |  |  |  | D.4.9 |  |
|  |  |  |  | D.4.10 | Places the plates, strips, and sized tablets on the band, through the inlet. |
|  |  |  |  | D.4.11 | Ensures the band moves forward, and performs the honing procedure. |
|  |  |  |  | D.4.12 | Removed the honed material from the outlet of the machine, and checks it. |
|  |  |  |  | D.4.13 | Directs the stone to the next point of procedure, if the honing procedure is completed. |
|  |  |  |  | D.4.14 | Directs the stone to the honing line again, provided that there are any deficiencies in honing. |
|  |  | D.5 | To burn surface by fire | D.5.1 | Contributes to bringing the plates, strips, and sized tablets, to be treated by burning, to the feeding part of the burning machine. |
|  |  |  |  | D.5.2 | Places the tablets on the inlet of the machine. |
|  |  |  |  | D.5.3 | Adjusts the fire outlet valve, thickness of the fire, blowing intensity, and the distance to the stone. |
|  |  |  |  | D.5.4 | Runs the machine, and places the stone on the proceeding band. |
|  |  |  |  | D.5.5 | Gives forward movement to the band, and ensures that the surface to be burned to contact with the fire. |
|  |  |  |  | D.5.6 | Adjusts the movement speed of the stone, as well as the speed of the fire when it is moving right and left. |
|  |  |  |  | D.5.7 | Performs surface burning procedure. |
|  |  |  |  | D.5.8 | Removes the stone from the outlet, and checks it. |
|  |  |  |  | D.5.9 | Directs the stone to the next treatment point, provided that the burning procedure is successfully completed. |
|  |  |  |  | D.5.10 | Directs the stone to the burning machine inlet, provided that there is a defect in the burning procedure. |
|  |  | D.6 | To treat surface with acid | D.6.1 | Contributes to bringing plates, strips, and sized tablets to be treated with acid, to the application bench. |
|  |  |  |  | D.6.2 | Covers the parts of the surface, which s/he does not want to expose to acid, with a material not affected by the acid. |
|  |  |  |  | D.6.3 | Adjusts the intensity of acids' affecting the surface, by diluting the hydrochloric acid to a value of %50 - %70. |
|  |  |  |  | D.6.4 | Brushes the diluted acid on the area to be treated. |
|  |  |  |  | D.6.5 | Waits until foaming, which surface as a result of the effect of acid, is over. |
|  |  |  |  | D.6.6 | After foaming, cleans the surface by flushing it. |
|  |  |  |  | D.6.7 | Checks the stone, directs the stone to the next point of procedure, if the procedure is completed. |
|  |  |  |  | D.6.8 | Re-adjusts the dilution degree of acid, and applies surface treatment procedure with acid again, provided that the impact on the stone is not effectual. |

|  |  | D.7 | To treat surface with brush | D.7.1 | Replaces the abrasive polishing heads with the abrasive brushes, which are used to ensure the intended surface shape, in strip tablet and tablet polishing machines. |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | D.7.2 | Contributes to bringing the plates, strips, and sized tablets, to be treated by brushing, to the feeding part of the brushing machine. |
|  |  |  |  | D.7.3 | Adjusts the pressure intensity to be applied by the brushes on the stone, and ensures that they descend on the surface of the stone. |
|  |  |  |  | D.7.4 | Turns on the fresh water spraying valve, on the band. |
|  |  |  |  | D.7.5 | Ensures the band to move, starts the brushing procedure. |
|  |  |  |  | D.7.6 | Observes the calibration and brushing heads through the open covers, throughout the brushing procedure, and checks how they work. |
|  |  |  |  | D.7.7 | Checks the strips and sized tablets, brushing treatments of which are finished. |
|  |  |  |  | D.7.8 | Directs the stones to the next point of process, if the brushing procedure was completed as expected. |
|  |  |  |  | D.7.9 | Applies brushing procedures on the stone again, provided that the brushing impact was not ensured as expected. |
|  |  | D.8 | To burst the surface | D.8.1 | Contributes to bringing the sized tablets, which are cut in 4 cm or in greater sizes, to the bursting machine. |
|  |  |  |  | D.8.2 | Positions the broad surface of the stone to be burst adjacent to gauge edge. |
|  |  |  |  | D.8.3 | Pushes the stone forward to the stone breaking edge, ensuring that it is adjacent to gauge edge. |
|  |  |  |  | D.8.4 | Continues this procedure until the whole stone surface is broken by the breaker. |
|  |  |  |  | D.8.5 | Bursts the part under the stone, which is not burst, without changing the surface that contacting the gauge. |
|  |  |  |  | D.8.6 | Places the stone on the pallet, if the required impact was ensured. |
|  |  |  |  | D.8.7 | Applies bursting procedure again on the parts which are not burst, provided that the intended impact is not achieved. |

|  |  | D.9 | To indent the surface | D.9.1 | Contributes to bringing the strips or sized tablets, to the machine usage area. |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | D.9.2 | Inserts adequate number of indenting disc to the machine, according to the number of indention. |
|  |  |  |  | D.9.3 | Adjusts the indention dept, on the control panel. |
|  |  |  |  | D.9.4 | Places the tablets to be indented on the machine inlet. |
|  |  |  |  | D.9.5 | Moves the band forward. |
|  |  |  |  | D.9.6 | Turns on the valve for spraying water, on the surface. |
|  |  |  |  | D.9.7 | Places the stones, indention procedures of which are completed, on the pallet. |

|  |  | D.10 | To fill the surface | D.10.1 | Contributes to bringing the plates, strips and sized tablets, to be filled, to the machine usage area. |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | D.10.2 | Fills the filling tank of the machine with the filling material to be used. |
|  |  |  |  | D.10.3 | Places plates, strips, and sized tablets on the conveyor band. |
|  |  |  |  | D.10.4 | Adjusts the pressure to be applied by the wipers on the surface, and check their work. |
|  |  |  |  | D.10.5 | Turns on the material valve, and ensures the filling material pour on the surface. |
|  |  |  |  | D.10.6 | Moves the band forward, and ensures that the filling procedure is done. |
|  |  |  |  | D.10.7 | Checks the stones, on which procedure is applied. |
|  |  |  |  | D.10.8 | Places the stone on the pallet, if the required impact was ensured. |
|  |  |  |  | D.10.9 | Completes the filling procedure by hand, provided that the intended impact is not ensured. |

|  |  | D.11 | To perform ageing procedure using drum and vibrator | D.11.1 | Contributes to bringing the strips or sized tablets, to the machine usage area. |
| --- | --- | --- | --- | --- | --- |
|  |  |  |  | D.11.2 | Places the strips or sized tablets, according to the tank capacity of the vibrator or drum. |
|  |  |  |  | D.11.3 | Places the grinding stones on tank. |
|  |  |  |  | D.11.4 | Sets the ageing time according to the hardness of the material to be aged. |
|  |  |  |  | D.11.5 | Runs the vibrator and the drum. |
|  |  |  |  | D.11.6 | Empties the tanks, when the ageing time is over. |
|  |  |  |  | D.11.7 | Checks the quality of ageing. |
|  |  |  |  | D.11.8 | Directs the stone to the next point of procedure, provided that the intended effect is ensured. |
|  |  |  |  | D.11.9 | Directs the stone to ageing procedure again, provided that the intended effect is not ensured. |

| Duties | Tasks | Performance Criteria |
| --- | --- | --- |
| Code | Title | Code | Title | Code | Description |
| F | To participate in vocational development activities | F.1 | To conduct studies on personal vocational development | F.1.1 | Participates in trainings organized by the operation and keeps the documents s/he received. |
|  |  |  |  | F.1.2 | Follows technological developments at the profession and the sector such as new appliances, new methods and new systems through periodicals, internet, journals etc. |
|  |  |  |  | F.1.3 | Conveys his/her knowledge and experiences to his/her co-workers. |
|  |  |  |  | F.1.4 | Observes installation and testing phases of newly-installed systems at the operation from the aspect of tasks of his/her duties. |

3.2.	Tools, Appliances and Equipment Used

1.	Polishing line (strip-plate)

2.	Weighing Machine

3.	Communication tools (radio, telephone etc.)

4.	Generator

5.	Truck

6.	Forklift

7.	Consumables (socket etc.)

8.	Personal Protective Equipment (safety helmet, boot, earflap, eye-glass, dust glass, dust machine, work shoes, protective gloves, overalls etc.)

9.	Warning signs and boards

10.	Plumb, laser

11.	Basic hand tools (voltage tester, screwdriver, hammer and wrench set etc.)

12.	Internal crane

13.	Auxiliary tools and materials (steel meter, water hose, pickaxe, shovel, sledge hammer, bucket, jimmy, chisel, jerry can, thick rope, rope, waterproof pen, non-wettable label, chock, cotton waste, styropor etc.)

14.	Pallet

15.	Metal stand

16.	Honing machine,

17.	Sanding machine,

18.	Hammering machine,

19.	Indentation machine,

20.	Filling machine,

21.	Surface polishing machine,

22.	Burning machine,

23.	Acid treatment machine,

24.	Brushing machine

3.3.	Knowledge & Skills

1.	Knowledge on emergency situation

2.	Knowledge on tools, apparatus and equipment

3.	Knowledge and skill of basic first aid

4.	Knowledge and skill of computer usage

5.	Knowledge on land use

6.	Knowledge and skill of drawing

7.	Skill of working in a team

8.	Knowledge and skill of using hand tools

9.	Manual skill

10.	Visual skill

11.	Ability of persuasion

12.	Oral and written communication skill

13.	Knowledge on human psychology

14.	Knowledge on Occupational Health and Safety

15.	Knowledge on the work site operation procedures

16.	Basic knowledge on quality assurance systems

17.	Ability of decision making

18.	Knowledge on use of user's guide, handbook and maintenance book

19.	Knowledge on materials

20.	Ability of distance and weight estimation

21.	Knowledge on legal regulations regarding the occupation

22.	Basic knowledge of electricity

23.	Basic knowledge of physics

24.	Basic knowledge of mathematics

25.	Knowledge on occupational and technological advancements

26.	Knowledge of vocational terms

27.	Ability of note taking

28.	Ability of working in a team or an organization

29.	Skill of learning and being able to share what s/he learned

30.	Ability to learn and teach

31.	Knowledge on measuring and control

32.	Ability to planning and problem solving

33.	Knowledge of color

34.	Knowledge on standard materials

35.	Knowledge and skill on technical drawing

36.	Knowledge on warning sign and table

37.	Knowledge on product

38.	Knowledge on fire fighting techniques and use of fire-extinguisher

39.	Knowledge on spare parts and consumables

40.	Knowledge of surface

3.4.	Attitudes and Behaviors

1.	To be cold blooded and calm under emergency and stressful situations

2.	To pay attention to use of appliances and consumables

3.	To be researcher

4.	To be hardworking

5.	To be able to use working time effectively and efficiently in compliance with work orders and instructions

6.	To be sensitive to protection of environment

7.	To adopt environmental, quality and OHS rules

8.	To be open to change and to adapt to changing conditions

9.	To pay attention to details

10.	To be attentive

11.	To be honest

12.	To be in harmony with the team

13.	To be open to criticism

14.	To be energetic

15.	To be observer

16.	To be cheerful

17.	To take initiatives

18.	To take care of human relations

19.	To have working discipline

20.	To pay attention to work safety

21.	To obey the working principles of the workplace

22.	To pay attention to cleaning, tidiness and workplace organization

23.	To pay attention to the usage of tools, appliances and equipments belonging to workplace

24.	To pay attention to quality

25.	To be decisive

26.	To be willful to improve himself/herself

27.	To ensure his/her own safety and safety of other people

28.	To have professional ethics

29.	To be planned and organized

30.	To be sensitive to issues of risk and hazard factors

31.	To be patient

32.	To take care of his/her own health

33.	To know his/her responsibilities and to fulfill the same

34.	To learn instructions and guides and to comply them meticulously

35.	To give fast and right reaction in dangerous situation in his/her own movement area

36.	To be clean

37.	To inform superiors properly and in time

38.	To share information clearly, effectively at shift change

39.	To be open to innovations

40.	To inform concerned people about the malfunctions which are not under his/her authority

4. TESTING, ASSESSMENT AND CERTIFICATION

Testing and assessment for certification with respect to national qualifications based on marble natural stone surface treatment worker (Level 3) Occupational Standard shall be held in written and/or oral forms, theoretically and practically, in testing and assessment centers where required conditions are met.

Testing and assessment method and practice principles shall be detailed with national qualifications to be drawn up pursuant to this occupational standard. Activities regarding testing, assessment and certification shall be conducted within the framework of Vocational Qualification Authority, Testing and Certification Regulation.

Note: This part shall not be published on the Official Gazette, shall only be included on the web site of VQA.

Annex: Institutions participated in the Occupational Standard Preparation Process

……….